### General Information

Our gold paint is a water based 2-pack metallic paint which has specifically been developed for the floral sector as a dipping paint or flower paint. Our gold bronze paint can however serve many decorative paint purposes and can also be applied by spray gun, brush or roller on different substrates such as interior walls, wood, metal, plastics, glass, and terra cotta.
The 2 components of this two-pack coating system are the following:

1. K-BIND 33
Being a high gloss concentrated binder.

2. K-STAB Bronze Paste (component 2) 
Being a gold effect pigment concentration, 
stabilized for water based systems and supplied as a dust-free paste dispersion.

Our bronze pastes are available in Rich, Rich Pale, Pale and Copper Gold.

### PRODUCT ADVANTAGES

Our water based coating system eliminates the use of hazardous thinners or solvents (like acetone) and offers excellent working properties, combined with high brilliance, good adherence and coating elasticity.

The durability of the metallic effect after application non-tarnishing effect will be there, depending on the exposure to the sun, the humidity conditions and the proportion of K-BIND or K-SPERSE AQ used in the end formulation.

### Stability & Storage

When prepared in excess quantities, a "gold" dipping bath is re-usable during a period of two weeks after its preparation.

Both components have as separate products a stability of min. 6 months, provided they are stored in their original sealed packaging, away from direct exposure to the sun and at temperatures between + 5° and + 40°C.

#### Packing

binder is available in 10 KG ,25 and 100 kg containers.
The K-stab bronze pastes are available in 5 KGS ,10 Kg PACK.

#### MSDS

Although both components of our 2-pack system are non-dangerous / non-hazardous products, please do consult the MSDS of both products prior to their handling.

#### Formulations:

| Formulation for DRIED flowers/absorbent material | Formulation for FRESH foliage/rapallent material |
| --- | --- |
| 1 part (9,09%) | k-stab bronze paste | 1 part | K-STABbronze paste |
| 1 part (9,09%) | K-BIND | 1 part | K-BIND |
| 9 parts (81,82%) | Water | 5-7 parts | Water |
| PREPARATION | PREPARATION |
| Step 1 | Obtain a homogeneous dispersion by mixing 2 parts of water with 1 part of K-STAB Bronze Paste. | Step 1 | Obtain a homogeneous dispersion by mixing 2 parts of water with 1 part of K-STAB Bronze Paste. |
| Step 2 | Add 1 part of K-BIND and mix gently. | Step 2 | Add 1 part of K-BIND and mix gently. |
| Step 3 | Add 7 parts of water and mix gently | Step 3 | Add remaining parts of water and mix gently |

"Parts" are to be understood as "parts by weight".  Use a stirrer which does not exceed 50 RPM in order to avoid the formation of foam and to obtain an optimal metallic effect.

#### Drying Time

Dust dry: 10-15 minutes, Touch dry: 20-30 minutes.

#### Film Forming

In cases where an increased film forming is required (to avoid an early oxidation/tarnishing of the metallic pigments which may occur in extreme humidity conditions) or when an increased rub resistance is required, a higher proportion of K-BIND  may have to be added in the formulation.

#### Difficult Species

95% of all flower and plant species do not require any surface preparation and will be perfectly coated when dipped as such.
Some very resilient species with a water repellent or fatty surface, will require a pre-dipping in a 80° C. water bath or 2 dipping sessions with a 10 minutes interval.

Contact us for more information

Surface_spl@yahoo.co.in

Or call 91-9830665596