| SILICON ALKYD BASED ---Clear coating (60% Solid) |  |
| --- | --- |
| Sil-alkyd (60% solid) |  | 100 |
| O-xylene (solvent) |  | 0 |
| Cobalt Octoate |  | 0.3 |
| Zirconium Octoate |  | 1.3 |
| Calcium Naphthenate |  | 1 |
| Total |  | 102.6 |